| NO. | TECHNICAL DESCRIPTION | REQUIREMENTS DATA |
| --- | --- | --- |
| 1 | Solar cells | Mono crystalline |
| 2 | Type of module | Bifacial dual glass / N-Type / Half cell |
| 3 | Standard | IEC61215/IEC61730/IEC61701/IEC62716 |
| 4 | Peak power watts-PMAX (STC) | 720 Wp |
| 5 | Max. Power Voltage (Vmpp) | 41.3 V |
| 6 | Max. Power Current (Impp) | 17.44 A |
| 7 | Open Circuit Voltage (Voc) | 49.4 V |
| 8 | Short Circuit Current (Isc) | 18.49 A |
| 9 | module efficiency | 23.2% |
| 10 | Temperature coefficient of PMAX | -0.29%/°C |
| 11 | Power output tolerance | 0 ~ +5W |
| 12 | Frame | 33mm Anodized Aluminum Alloy |
| 13 | Product warranty | 12 year Product Workmanship Warranty |
| 14 | Linear power output warranty | 30 year Power Warranty |
| 15 | First-year power degradation | ≤1% |
| 16 | Annual power attenuation | ≤0.45% |
| 17 | Operational temperature | -40~+80ºC |
| 18 | Maximum system voltage | 1500V DC |
| 19 | Connector | TS4 /TS4 Plus |
| 20 | Mechanical performance | up to 5400 Pa positive load and 2400 Pa negative load |
| 21 | Degree of protection (module) | IP68 |
| 22 | Degree of protection (J-Box) | IP68 |
| 23 | Front Glass | 2.0 mm Heat Strengthened Glass, High Transmission, anti relective Coating |
| 24 | Back Glass | 2.0 mm Heat Strengthened Glass |
| 25 | Encapsulant material | POE/EVA |
| 26 | Installation Method | Both Landscape/Portrait methods |

Technical Specifications of the Panel